| 喷丸工艺规程（首页）SHOT PEENING PLANNING SHEET（FIRST PAGE） |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 项目 ITEM | C909 （1） |  |  |  | 工艺规程编号 P/S No. |  |  | 554A1010-001-001 （2） |  |  |  |  |  | 工艺规程版次 P/S REV. |  | A （3） | 厂代号SHOP No. |  |  | 15 （4） | 零件数量 PART QTY. |  | ≤6 （5） |
| 零/组件名称 P/S NAME |  | 零/组件版次 P/S REVISION |  |  |  | 材料牌号及状态 MAT’L. DESG. CON |  |  |  | 材料标准 MAT’L SPEC. |  |  |  |  | 机床型号及编号 MACHINE TYPE and No. |  |  |  | 要求的喷丸强度REQUIRED INTENSITY |  |  | 要求的覆盖率 REQUIRED COVERAGE |  |
| 铰链接头 （6） |  | DA （7） |  |  |  | 7075-T7352 （8） |  |  |  | AMS-A-22771 （9） |  |  |  |  | PRTRAT-4SM-G7(9540)（10） |  |  |  | 0.15-0.25mmA （11） |  |  | 100% （12） |  |
| 弹丸种类及标准 SHOT TYPE and SPEC. |  |  |  | 弹丸号 SHOT No. |  |  |  |  | 喷嘴数量 NOZZLE QTY. |  |  | 喷嘴尺寸 NOZZLE SIZE |  |  | 喷丸区域 SHOT PEENING AREA |  |  |  | 实际喷丸强度 ACTUAL INTENSITY |  |  | 零件最小厚度 MIN.THICKNESS |  |
| 铸钢 AMS2431/2 （13） |  |  |  | ASH280 （14） |  |  |  |  | 2个 （15） |  |  | 内径φ8mm±5%（16） |  |  | 所有表面 （17） |  |  |  | 0.201mmA 0.178 mmA （18） |  |  | N/A （19） |  |
| 喷丸次数或时间 PEENING TIME OR CYCLES |  |  |  | 喷丸角度 IMPINGEMENT ANGLE |  |  |  |  | 零件进给速度 FEED RATE for PART |  |  | 喷射距离 SPRAY DIS. |  |  | 零件分类 PART CLASS |  |  |  | 试片类型及标准 STRIP TYPE and SPEC. |  |  | 试片数量 TEST STRIP QTY. |  |
| 1次 （20） |  |  |  | 45°（0°～+10°）（21） |  |  |  |  | 750mm/min±10%（22） |  |  | 250mm±10% （23） |  |  | 一般件 （24） |  |  |  | A型（SAE J442） （25） |  |  | 5+5 （26） |  |
| 弹丸流量 SHOT FLOW RATE |  |  |  | 空气压力 AIR PRESSURE |  |  |  |  | 夹具编号 FIXTURE No. |  |  | 零件验证工具号 PVT No. |  |  | 遮盖夹具号 MASKING TOOLS No. |  |  |  | 机床程序 MACHINE PROGRAM |  |  | 引用文件 DOCUMENTS REF. |  |
| 15.0lbs/min±10% （27） |  |  |  | 1#15.0PSI±10% 2#18.0PSI±10%（28） |  |  |  |  | SPF-08-16 |  |  | SPF-08-25-1 |  |  | N/A |  |  |  | O1133(A) |  |  | CPS6600 |  |
|  |  |  |  |  |  |  |  |  | N/A |  |  | N/A |  |  | N/A |  |  |  | O1134(A) |  |  | S25-I00803-1 |  |
|  |  |  |  |  |  |  |  |  | （30） |  |  | （31） |  |  | （32） |  |  |  | （33） |  |  | （34） |  |
| 喷嘴震动速度 OSCILLATION SPEED |  |  |  | N/A （29） |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 图纸 DRW. |  |  |  |  |  |  |  |  |  |  | 零件表 P.L. |  |  |  |  |  |  | 图纸更改单DRW.CHANGE NOTE |  |  |  |  |  |
| 图号DRW. No. |  |  |  |  | 页次PAGE |  | 版次REV. |  |  |  | 代号CODE |  |  |  | 版次REV. |  |  | 更改单号CHANGE NOTE No. |  |  |  | 版次REV. |  |
| N/A |  |  |  |  | N/A |  | N/A |  |  |  | DPL554A1010-001-001 |  |  |  | DA |  |  | N/A |  |  |  | N/A |  |
| （35） |  |  |  |  | （36） |  | （37） |  |  |  | （38） |  |  |  | （39） |  |  | （40） |  |  |  | （41） |  |
| 编制 DEVELOPED BY |  |  | 校对 CHECKED BY |  |  |  |  | 审核 REVIEWED BY |  |  |  |  | 质保 Q.A. |  |  | 批准 APPROVED BY |  |  |  | 客户 CUSTOMER BY |  | 更改单号 CHANGE NOTE No. |  |
| 张一2025.8.25 （44） |  |  | 李二2025.8.25（45） |  |  |  |  | 王三2025.8.25 （46） |  |  |  |  | 张四2025.8.25 （47） |  |  | 李五2025.8.25 （48） |  |  |  | 刘六2025.8.25（49） |  | ARJ-ZLG7010-5 （43） |  |

第 ( ) 页   共( )页（42）

PAGE   OF

填写说明Instructions for Filling：

- 生产厂工艺员填写项目名称。

The process engineer of production plant fills in the project.

- 生产厂工艺员填写工艺规程编号。

The process engineer of the production plant fills in the process specification number.

- 生产厂工艺员填写工艺规程版次。

The process engineer of the production plant fills in the version of the process specification.

- 生产厂工艺员填写厂代号。

The process engineer of production plant fills in the plant code.

- 生产厂工艺员填写一次可同时进行喷丸的最多零件数量。

The process engineer of production plant fills in the maximum number of parts that can be shot blasted simultaneously at one time.

- 生产厂工艺员填写零/组件名称。

The process engineer of production plant fills in the name of the component/part.

- 生产厂工艺员填写零/组件版次。

The process engineer of the production plant fills in the version of the parts/components.

- 生产厂工艺员填写零/组件材料牌号及状态。

The process engineer of the production plant fills in the material grade and status of the parts/components.

- 生产厂工艺员填写零/组件材料标准。

The process engineer of the production plant fills in the material standards for parts/components.

- 生产厂工艺员填写喷丸的机床型号及编号。

The process engineer of production plant fills in the machine model and number for shot blasting.

- 生产厂工艺员填写要求的喷丸强度。

The production plant process technician fills in the required shot peening intensity.

- 生产厂工艺员填写要求的覆盖率。

The process engineer of production plant fill in the required coverage rate.

- 生产厂工艺员填写弹丸种类及标准。

The process engineer of production plant fills in the type and standard of the projectile.

- 生产厂工艺员填写弹丸号。

The process engineer of production plant fills in the bullet number.

- 生产厂工艺员填写喷嘴数量。

The process engineer of production plant fills in the number of nozzles.

- 生产厂工艺员填写喷嘴尺寸。

The process engineer of production plant fills in the nozzle size.

- 生产厂工艺员填写喷丸区域。

The process engineer of production plant fills in the shot blasting area.

- 生产厂工艺员填写实际喷丸强度。

The process engineer of production plant fills in the actual shot peening intensity.

- 生产厂工艺员填写零件最小厚度，不适用时填写N/A。

The process engineer of production plant shall fill in the minimum thickness of the parts, and if not applicable, fill in N/A.

- 生产厂工艺员填写喷丸次数或时间。

The process engineer of the production plant shall fill in the number or time of shot blasting.

- 生产厂工艺员填写喷丸角度。

The process engineer of production plant fills in the shot blasting angle.

- 生产厂工艺员填写零件进给速度。

The process engineer of production plant fill in the part feed rate..

- 生产厂工艺员填写喷射距离。

The process engineer of production plant fills in the spraying distance.

- 生产厂工艺员填写零件分类。

The process engineer of production plant fills in the part classification.

- 生产厂工艺员填写试片类型及标准。

The process engineer of production plant fills in the type and standard of the test piece.

- 生产厂工艺员填写试片数量。

The process engineer of production plant fills in the quantity of test pieces.

- 生产厂工艺员填写弹丸流量。

The process engineer of production plant fill in the projectile flow rate.

- 生产厂工艺员填写空气压力。

The process engineer of production plant fills in the air pressure.

- 生产厂工艺员填写夹具编号，不适用时填写N/A。

The process engineer of the production plant shall fill in the fixture number, and if not applicable, fill in N/A.

- 生产厂工艺员填写夹具编号，不适用时填写N/A。

The process engineer of the production plant shall fill in the fixture number, and if not applicable, fill in N/A.

- 生产厂工艺员填写零件验证工具号，不适用时填写N/A。

The process engineer of the production plant shall fill in the part verification tool number, and if not applicable, fill in N/A.

- 生产厂工艺员填写遮盖夹具号，不适用时填写N/A。

The process engineer of production plant shall fill in the cover fixture number, and if not applicable, fill in N/A.

- 生产厂工艺员填写机床程序。

The process engineer of production plant fills in the machine tool program.

- 生产厂工艺员填写引用文件，如工艺规程和典型工艺规程等。

The process engineer of production plant fill in reference documents, such as process specifications and typical process specifications.

- 生产厂工艺员填写引用的图纸的图号，不适用时填写N/A。

The process engineer of the production plant shall fill in the drawing number of the referenced drawing, and if not applicable, fill in N/A.

- 生产厂工艺员填写引用的图纸的页次，不适用时填写N/A。

The process engineer of production plant shall fill in the page number of the referenced drawings, and if not applicable, fill in N/A.

- 生产厂工艺员填写引用的图纸的版次，不适用时填写N/A。

The process engineer of production plant shall fill in the version of the referenced drawings, and if not applicable, fill in N/A.

- 生产厂工艺员填写引用的零件表号，不适用时填写N/A。

The process engineer of production plant shall fill in the referenced part list number, and if not applicable, fill in N/A.

- 生产厂工艺员填写引用的零件表版次，不适用时填写N/A。

The process engineer of the production plant shall fill in the version of the referenced parts list, and if not applicable, fill in N/A.

- 生产厂工艺员填写引用的图纸更改单编号，不适用时填写N/A。

The process engineer of the production plant shall fill in the reference drawing change order number, and if not applicable, fill in N/A.

- 生产厂工艺员填写引用的图纸更改单半次，不适用时填写N/A。

The process engineer of production plant shall fill in the referenced drawing change form half a time, and if not applicable, fill in N/A.

- 生产厂工艺员本页所在页次及总页数。

The page number and total number of pages for The process engineer of production plant on this page.

- 当适用时，生产厂工艺员填写工艺规程更改单号。

When applicable, The process engineer of production plant shall fill in the process specification change order number.

- 生产厂工艺员签名并填写日期。

The process engineer of the production plant shall sign and indicate the date.

- 生产厂工艺员签名并填写日期。

The process engineer of the production plant shall sign and indicate the date.

- 生产厂技术室主任签名并填写日期。

The director of the technical department of the production plant shall sign and indicate the date.

- 质量工程室技术员/主任签名并填写日期。

The technician/director of the Quality Engineering Department shall sign and indicate the date.

- 生产厂技术厂长签名并填写日期。

The technical director of the production plant shall sign and indicate the date.

- 当客户有要求时，由客户签名并填写日期。

When requested by the customer, the customer shall sign and indicate the date.